**\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

**ARCHITECTURE, ENGINEERING AND CONSTRUCTION**



ARCHITECTURE & ENGINEERING

326 East Hoover, Mail Stop B

Ann Arbor, MI 48109-1002

Phone: 734-764-3414

Fax: 734-936-3334

BuildingName  
The Description of the Project  
P00000000 0000

DOCUMENTS

SPECIFICATION DIVISION 31

NUMBER SECTION DESCRIPTION

DIVISION 31 EARTHWORK

SECTION 312326 – FLOWABLE FILL

END OF CONTENTS TABLE

1. DIVISION 31 EARTHWORK
   1. SECTION 312326 – FLOWABLE FILL
      1. GENERAL

THIS SECTION SPECIFIES A PUMPABLE CONCRETE GROUT MATERIAL WITH LIMITED SHRINKAGE - USED IN SPECIAL CIRCUMSTANCES ONLY.

* + - 1. SUMMARY
         1. Work Included: Class A Compacted Fill as indicated on drawings.

In addition, install embedded items furnished under Division 05 Section "Metal Fabrication".

* + - 1. SUBMITTALS
         1. Submittals: In addition to product data, submit proposed mix design, including slump and weight data; and copy of laboratory test report showing strengths achieved and expected curing time.
    1. PRODUCTS
       1. ACCEPTABLE MANUFACTURERS
          1. Manufacturer: Provide materials manufactured by the following:

Flo-Fill Co., 1008 Scheurmann St., Essexville, Mi 48732; phone no. (517)-893-1493.

"Flo-Fill" compacted, class A, fill; complying with the following:

Fly Ash: approximately 1950 pounds per cubic yard.

Portland cement: approximately 85 pounds per cubic yard.

Water: 60 to 70 gallons per cubic yard.

Minimum Cured Strength: 6000 pounds per square foot.

Dry Weight: 60 to 70 pounds per cubic foot.

* + - 1. MIXING
         1. Mix material on site in strict accordance with manufacturer's instructions.
    1. EXECUTION
       1. INSTALLATION
          1. Placing: Pump mixture into place in fluid state to eliminate compaction effort. Spread and level to grades indicated on drawings.
          2. Curing: Cure by drying for a minimum of 7 calendar days before placing additional construction over fill material.

END OF SECTION 312326